| # CHEMICAL TESTED (受 測 化 學 物 質) | CAS NUMBER | STANSOLV® NITRILE |  |  |  |  |  |  | ## STANZOIL®NEOPRENE |  |  |  |  |  |  | ## NATURAL RUBBER |  |  |  |  |  |  | ## PYLOX®PVC |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | DEGRADATION RATING |  |  |  | PERMEATION BREAKTHROUGH |  |  | DEGRADATION RATING |  |  |  | PERMEATION BREAKTHROUGH |  |  | DEGRADATION RATING |  |  |  | PERMEATION BREAKTHROUGH |  |  | DEGRADATION RATING |  |  |  | PERMEATION BREAKTHROUGH |  |  |
|  |  | Time In Min. |  |  |  | BTT | LDL | Rate | Time In Min. |  |  |  | BTT | LDL | Rate | Time In Min. |  |  |  | BTT | LDL | Rate | Time In Min. |  |  |  | BTT | LDL | Rate |
|  |  | 5 | 30 | 60 | 240 | Min. | PPM |  | 5 | 30 | 60 | 240 | Min. | PPM |  | 5 | 30 | 60 | 240 | Min. | PPM |  | 5 | 30 | 60 | 240 | Min. | PPM |  |
| 1.ACETALDEHYDE 乙醛 | 75-07-0 | NT |  |  |  | NT |  |  | E | E | E | E | 21 | .1 | 108 | E | E | E | E | 2 | .4 | 78 | NT |  |  |  | NT |  |  |
| 2.ACETIC ACID GLACIAL 冰醋酸 | 64-19-7 | NT |  |  |  | 118 | .1 | 1326 | NT |  |  |  | NT |  |  | NT |  |  |  | 21 | .1 | 12 | NT |  |  |  | 85 | .1 | 1.8 |
| 3.ACETIC ACID 50% 50% 醋酸 | 64-19-7 | E | E | E | E | >480 | .02 | ND | E | E | E | E | >480 | .1 | ND | E | E | E | E | 31 | .02 | 18 | E | E | E | E | 47 | .02 | 0.36 |
| 4.ACETONE 丙酮 | 67-64-1 | G | P | P | P | NT |  |  | E | E | E | E | 12 | - | 210 | E | E | E | E | 7 | .05 | 30 | G | P | P | P | <1 | - | # |
| 5.ACETONITRILE 乙 | 75-05-8 | NT |  |  |  | NT |  |  | E | E | E | E | 40 | - | 42 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 6.ACRYONITRILE 丙烯 | 107-13-1 | P | P | P | P | 12 | .001 | >50 | E | G | G | G | 40 | .07 | >50 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 7.AMMOUIUM HYDROXIDE 29% 氫氧化銨 | 1336-61-6 | E | E | E | E | >480 | 1.0 | ND | E | E | E | E | >480 | 1.0 | ND | E | E | E | E | 58 | 1.0 | 108 | E | E | E | E | >480 | 1.0 | ND |
| 8.ANILINE 苯胺 | 62-53-3 | G | G | P | P | 72 | .001 | 18 | E | E | E | E | >480 | .005 | ND | E | E | E | E | >480 | .008 | ND | E | E | G | G | >480 | .009 | ND |
| 9.AROCLOR 1254(50%PCB/50%TCB) |  | NT |  |  |  | 343 | 1.0 | 216 | NT |  |  |  | >480 | 1.0 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 10.BENZENE 苯 | 71-43-2 | E | F | P | P | 27 | .03 | 582 | NT |  |  |  | 16 | - | 798 | NT |  |  |  | NT |  |  | NT |  |  |  | 2 | - | 1500 |
| 11.BENZENE CHLORIDE 氯苯 | 108-90-7 | NT |  |  |  | 15 | - | 960 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NF |  |  |
| 12.BIS (2-HYDROXYETHYL) AMINE 二醇胺 | 111-42-2 | E | E | E | E | .480 | 1.1 | ND | E | E | E | E | >480 | 1.1 | ND | E | E | E | E | >480 | 1.1 | ND | E | E | E | E | >480 | 1.1 | ND |
| 13.2-BUTANONE 2-丁酮 | 78-93-3 | NT |  |  |  | 6 | - | 522 | E | G | G | G | 22 | - | 930 | E | E | G | G | 6 | - | 522 | NT |  |  |  | 1 | - | # |
| 14.2-BUTOXYETHANOL 2-丁氧基乙醇 | 111-76-2 | E | E | E | E | >480 | .5 | ND | E | E | E | E | 147 | 1.0 | 30 | E | E | E | E | 12 | 1.0 | 162 | NT |  |  |  | NT |  |  |
| 15.BUTYL ACETATE 乙酸丁酯 | 123-86-4 | E | G | F | F | 101 | .1 | 144 | NT |  |  |  | 52 | - | 318 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 16.BUTYL CELLOSOLVE 丁基溶纖劑 | 111-76-2 | E | E | E | E | >480 | .5 | ND | E | E | E | E | 147 | 1.0 | 30 | E | E | E | E | 12 | 1.0 | 162 | NT |  |  |  | NT |  |  |
| 17.CARBOLIC ACID 碳酸 | 108-95-2 | NT |  |  |  | >480 | - | ND | E | E | E | E | >480 | .2 | ND | E | E | E | G | >480 | .06 | ND | NT |  |  |  | 32 | - | 78 |
| 18.CARBON DICHLORIDE 二氯化碳 | 127-18-4 | E | G | G | F | 373 | .0002 | 27 | NT |  |  |  | 28 | .0002 | 453 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 19.CARBON DISULFIDE 二硫化碳 | 75-15-0 | E | G | F | F | 20 | .2 | 516 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 20.CARBON TETRACHLORIDE 四氯化碳 | 56-23-5 | E | E | G | F | 341 | 1.0 | 48 | G | F | P | P | 31 | - | 1512 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 21.CELLOSOLVE 溶纖劑 | 110-80-5 | E | E | E | G | 416 | .03 | 24 | E | E | E | E | 352 | .06 | 18 | E | E | E | E | 10 | .03 | 12 | NT |  |  |  | NT |  |  |
| 22.CELLOSOLVE ACETATE 溶纖劑乙酸酯 | 111-15-9 | E | G | F | P | 162 | .1 | 72 | E | G | G | G | 76 | .07 | 252 | E | E | G | G | 13 | - | - | NT |  |  |  | NT |  |  |
| 23.CHLOROBENZENE 氯苯 | 108-90-7 | NT |  |  |  | 15 | - | 960 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 24.CHLOROFORM 氯仿 | 67-66-3 | NT |  |  |  | NT |  |  | F | P | P | P | 12 | .2 | 1368 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 25.CHLOROTHENE 氯辛 | 71-55-6 | F | P | P | P | 131 | .05 | 264 | F | P | P | P | 27 | - | 1182 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 26.0-CHLOROTOLUENE O-氯甲苯 | 95-49-8 | NT |  |  |  | 52 | - | 984 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 27.p-CHLOROTOLUENE P-氯甲苯 | 106-43-4 | NT |  |  |  | 25 | - | 888 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 28.CHROMIC ACID 50% 鉻酸 | 7738-94-5 | E | E | E | E | >175 | .1 | # | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | >480 | .1 | ND |
| 29.m-CRESOL (3-CRESOL) 3-甲氧基甲酚 | 108-39-4 | E | G | F | F | 210 | 5.0 | 126 | E | E | E | E | >480 | 5.0 | ND | E | E | E | G | 150 | 5.0 | 12 | E | E | E | E | 150 | 5.0 | 36 |
| 30.CUMENE 茴香素 | 98-82-8 | E | E | G | G | 271 | .03 | 48 | E | G | F | P | 41 | .4 | 216 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 31.CYCLOHEXANE 環己烯 | 110-82-7 | E | E | E | E | >480 | .02 | ND | E | E | E | E | 159 | .03 | 42 | NT |  |  |  | NT |  |  | NT |  |  |  | 16 | - | 102 |
| 32.DIAMINE 二胺 | 302-50-1 | E | E | E | E | >480 | .7 | ND | E | E | E | E | >480 | .7 | ND | E | E | E | E | 218 | .7 | 12 | E | E | E | E | >480 | .7 | ND |
| 33.1,2-DICHLOROBENZENE 1,2-二氯苯 | 95-55-01 | NT |  |  |  | 37 | - | 1140 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 34.1,3-DICHLOROBENZENE 1,3-二氯苯 | 541-73-7 | G | F | P | P | 73 | .3 | 174 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 35.DICHLORODIFLUOROMETHANE 二氯二氟甲烷 | 75-71-8 | NT |  |  |  | >480 | .08 | ND | NT |  |  |  | >480 | .03 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 36.1,2-DICHLOROETHANE 1,2-二氯乙烷 | 107-06-2 | P | P | P | P | 16 | .06 | 1752 | E | P | P | P | 33 | .09 | 1482 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 37.DICHLOROMETHANE 二氯甲烷 | 75-09-2 | NT |  |  |  | NT |  |  | G | F | F | F | 6 | - | 1434 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 38.DIETHANOLAMINE 二乙醇胺 | 111-42-2 | E | E | E | E | >480 | 1.1 | ND | E | E | E | E | >480 | 1.1 | ND | E | E | E | E | >480 | 1.1 | ND | E | E | E | E | >480 | 1.1 | ND |
| 39.DIETHYL ETHER 二乙基醚 | 60-29-7 | E | E | E | E | 64 | .1 | 78 | E | E | E | E | 18 | .1 | 486 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 40.1,4-DIETHYLENE DIOXIDE 1,4-環氧己烷 | 123-91-1 | NT |  |  |  | NT |  |  | NT |  |  |  | 28 | - | 372 | NT |  |  |  | NT |  |  | NT |  |  |  | 6 | - | 1500 |
| 41.DIMETHYL ACETAMIDE(DMAC) 二甲基乙醯胺 | 127-19-5 | G | P | P | P | 28 | .001 | # | E | G | G | P | NT |  |  | E | F | F | F | NT |  |  | G | # | # | # | 20 | .005 | # |
| 42.DIMETHYL FORMAMIDE 二甲基甲醯胺 | 68-12-2 | NT |  |  |  | 35 | .2 | 246 | E | E | E | E | 110 | .1 | 246 | E | E | E | E | 67 | .1 | 246 | NT |  |  |  | NT |  |  |
| 43.DIMETHYL SULFOXIDE 二甲基乙 | 67-68-5 | E | E | G | P | 0 | .004 | 6 | E | E | E | E | 0 | .004 | 0 | E | E | E | E | 240 | .004 | 0 | E | E | G | G | 60 | .004 | 0 |
| 44.1,4-DIOXANE 1,4-環氧己烷 | 123-91-1 | NT |  |  |  | NT |  |  | NT |  |  |  | 28 | - | 372 | NT |  |  |  | NT |  |  | NT |  |  |  | 6 | - | 1500 |
| 45.ETHANOL 乙醇 | 64-17-5 | E | E | E | E | >480 | .002 | ND | E | E | E | E | >480 | .002 | ND | E | E | E | E | >480 | .02 | ND | E | E | E | E | 20 | - | 30 |
| 46.2-ETHOXYETHANOL 溶纖劑 | 110-80-5 | E | E | E | G | 416 | .03 | 24 | E | E | E | E | 352 | .06 | 18 | E | E | E | E | 10 | .03 | 12 | NT |  |  |  | NT |  |  |
| 47.2-ETHOXYETHYL ACETATE 2-乙氧基乙基乙酸酯 | 111-15-9 | E | G | F | P | 162 | .1 | 72 | E | G | G | G | 76 | .07 | 252 | E | E | G | G | 13 | - | - | NT |  |  |  | NT |  |  |
| 48.ETHYL ACETATE 乙基乙酸酯 | 141-78-6 | NT |  |  |  | NT |  |  | E | G | G | G | 34 | .08 | 1068 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 49.ETHYL ALCOHOL (ETHANOL) 乙基醇 | 64-17-5 | E | E | E | E | >480 | .002 | ND | E | E | E | E | >480 | .002 | ND | E | E | E | E | >480 | .02 | ND | E | E | E | E | 20 | - | 30 |
| 50.ETHYL ETHER 乙基醚 | 74-96-4 | E | E | E | E | 64 | .1 | 78 | E | E | E | E | 18 | .1 | 486 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 51.ETHYLENE DICHLORIDE 二氯乙烯 | 107-06-2 | P | P | P | P | 16 | .06 | 1752 | E | P | P | P | 33 | .09 | 1482 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 52.ETHYLENE GLYCOL 乙二醇 | 107-21-1 | E | E | E | E | >480 | - | ND | E | E | E | G | >480 | - | ND | E | E | E | E | >480 | - | ND | E | E | E | E | >480 | - | ND |
| - ETHYLENE GYCOL MONETHYL ETHER ACETATE二甲氧基乙醇乙酸酯 | 111-15-9 | E | G | F | P | 162 | .1 | 72 | E | G | G | G | 76 | .07 | 252 | E | E | G | G | 13 | - | - | NT |  |  |  | NT |  |  |
| 54.ETHYLENE GYCOL MONOETHYL ETHER 2-甲氧基乙醇 | 110-80-5 | E | E | E | G | 416 | .1 | 72 | E | E | E | E | 352 | .06 | 18 | E | E | E | E | 10 | .03 | 12 | NT |  |  |  | NT |  |  |
| 55.ETHYLENE OXIDE 環氧乙烷 | 75-21-8 | NT |  |  |  | 32 | .3 | 126 | NT |  |  |  | 31 | 3.0 | 60 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 56.FORMALDEHYDE 37% 甲醛 | 50-00-0 | E | E | E | E | >480 | 8.0 | ND | E | E | E | E | >480 | 3.0 | ND | E | E | E | E | >480 | .01 | ND | G | G | G | G | >480 | .01 | ND |
| 57.FORMALIN SOLUTION 福馬林 | 50-00-0 | E | E | E | E | >480 | 8.0 | ND | E | E | E | E | >480 | 3.0 | ND | E | E | E | E | >480 | .01 | ND | G | G | G | G | >480 | .01 | ND |
| 58.FREON 12 氟氯烷12 | 75-71-8 | NT |  |  |  | >480 | .08 | ND | NT |  |  |  | >480 | .03 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 59.FREON TF 氟氯烷TF | 76-13-1 | E | E | E | E | >480 | .01 | ND | E | E | E | E | >480 | .2 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | 11 | - | 192 |
| 60.FURFURAL 糠醛 | 98-01-1 | P | P | P | P | 61 | .05 | >50 | E | E | F | F | 95 | .2 | >50 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 61.GASOLINE 汽油 | 8006-61-9 | E | E | E | E | >480 | .1 | ND | E | E | E | E | 96 | .2 | 96 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 62.HEPTANE 庚烷 | 142-82-5 | E | E | E | E | 2 | .01 | 0.018 | E | E | E | E | 124 | .02 | 12 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 63.HEXANE 己烷 | 110-54-3 | E | E | E | E | >480 | .08 | ND | E | E | E | E | 39 | .08 | 36 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 64.HYDRAZINE 聯胺 | 302-01-2 | E | E | E | E | >480 | .7 | ND | E | E | E | E | >480 | .7 | ND | E | E | E | E | 218 | .7 | 12 | E | E | E | E | >480 | .7 | ND |
| 65.HYDROCHLORIC ACID 37.5% (HCL) 鹽酸 | 7647-01-0 | E | E | E | E | >480 | .4 | ND | E | E | E | E | >480 | 4.0 | ND | E | E | E | E | 211 | 4.0 | 1308 | E | E | E | E | >480 | 4.0 | ND |
| 66.HYDROFLUORIC ACID 48% (HF) 氫氟酸 | 7664-39-3 | E | E | E | G | 134 | .001 | 30 | E | E | E | E | >480 | 1.0 | ND | E | E | E | E | >480 | 1.0 | ND | E | E | E | E | 110 | 1.0 | 0 |
| 67.ISOAMYL ACETATE 乙酸戊酯 | 123-92-2 | NT |  |  |  | NT |  |  | NT |  |  |  | 30 | - | 312 | NT |  |  |  | NT |  |  | NT |  |  |  | 5 | - | 1602 |
| 68.ISOBUTYL ALCOHOL 二丁基醇 | 78-83-1 | E | E | E | E | >480 | .01 | ND | E | E | E | E | >480 | .03 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 69.ISOPROPANOL (IPA) 異丙醇 | 67-63-0 | E | E | E | E | >480 | .05 | ND | E | E | E | E | >60 | .0006 | ND | E | E | E | E | >60 | - | ND | E | E | E | E | 208 | - | 0 |
| 70.ISOPROPYL ALCOHOL (ISOPROPANOL, IPA) 異丙醇 | 67-63-0 | E | E | E | E | >480 | .05 | ND | E | E | E | E | >60 | .0006 | ND | E | E | E | E | >60 | - | ND | E | E | E | E | 208 | - | 0 |
| 71.ISOPROPYL BENZENE 異丙苯 | 98-82-8 | E | E | E | G | 271 | .03 | 48 | E | G | F | P | 41 | 4 | 216 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 72.KEROSENE 煤油 | 8008-20-6 | E | E | E | E | >480 | .007 | ND | E | E | E | E | >480 | .00005 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 73.METHANE DICHLORIDE 二氯甲烷 | 75-09-2 | NT |  |  |  | NT |  |  | G | F | F | F | 6 | - | 1434 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 74.METHANOL 甲醇 | 67-56-1 | E | E | E | E | 118 | .08 | 18 | E | E | E | E | >60 | - | ND | E | E | E | E | >60 | - | ND | NT |  |  |  | 3 | - | 18 |
| 75.METHYL ALCOHOL (METHANOL) 甲基醇 | 67-56-1 | E | E | E | E | 118 | .08 | 18 | E | E | E | E | >60 | - | ND | E | E | E | E | >60 | - | ND | NT |  |  |  | 3 | - | 18 |
| 76.METHYL CHLOROFORM 甲基氯仿 | 71-55-6 | F | P | P | P | 131 | .05 | 264 | F | P | P | P | 27 | - | 1182 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 77.METHYL CYANIDE 乙 | 75-05-8 | NT |  |  |  | NT |  |  | E | E | E | E | 40 | - | 42 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 78.METHYL ETHYL KETONE (MEK) 甲基乙基酮 | 78-93-3 | NT |  |  |  | 6 | - | 522 | E | G | G | G | 22 | - | 930 | E | E | G | G | 6 | - | 522 | NT |  |  |  | 1 | - | # |
| 79.METHYL IODIDE 甲基碘化物 | 74-88-4 | NT |  |  |  | NT |  |  | NT |  |  |  | 12 | - | 3702 | NT |  |  |  | NT |  |  | NT |  |  |  | 1 | - | # |
| 80.METHYL ISOBUTYL KETONE (MIBK) 甲基異丁基酮 | 108-10-1 | G | P | P | P | 57 | .01 | >50 | F | P | P | P | 50 | .01 | >50 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 81.n-METHYL-2-PYRROLIDONE n-甲基2- 啶 | 872-50-4 | P | P | P | P | 108 | .01 | 24 | E | G | G | P | 448 | .01 | ,7 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 82.METHYLENE CHLORIDE 氯化乙烯 | 75-09-2 | NT |  |  |  | NT |  |  | G | F | F | F | 6 | - | 1434 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 83.m-METHYLPHENOL (3-METHYLPHENOL) m-甲酚 | 108-39-4 | E | G | F | F | 210 | 5.0 | 126 | E | E | E | E | >480 | 5.0 | ND | E | E | E | G | 150 | 5.0 | 12 | E | E | E | E | 150 | 5.0 | 36 |
| 84.MINERAL SPIRITS 礦物酒精 | 8030-30-6 | E | E | E | E | >480 | .02 | ND | E | E | E | E | 126 | .002 | 12 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 85.MURIATIC ACID 鹽酸 | 7647-01-0 | E | E | E | E | >480 | .4 | ND | E | E | E | E | >480 | 4.0 | ND | E | E | E | E | 211 | 4.0 | 1308 | E | E | E | E | >480 | 4.0 | ND |
| 86.NAPHTHA 揮發油 | 8030-30-6 | E | E | E | E | >480 | .02 | ND | E | E | E | E | 126 | .002 | 12 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 87.NITRIC ACID 50% 硝酸 | 7697-37-2 | E | G | G | P | 72 | .07 | 1206 | E | E | E | E | >480 | .0003 | ND | E | E | E | G | 233 | .1 | # | E | E | E | E | 114 | .08 | 0 |
| 88.NITROBENZENE 硝基苯 | 98-95-3 | G | P | P | P | 60 | 1.0 | 90 | E | E | G | P | 60 | 1.0 | 120 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 89.OLEIC ACID 油酸 | 112-80-1 | E | E | E | E | NT |  |  | E | E | E | E | NT |  |  | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 90.PENTANE 戊烷 | 109-66-0 | NT |  |  |  | NT |  |  | NT |  |  |  | 38 | - | 18 | NT |  |  |  | NT |  |  | NT |  |  |  | 9 | - | 102 |
| 91.PERCHLOROETHYLENE 四氯乙烯 | 127-18-4 | E | G | G | F | 373 | .0002 | 27 | NT |  |  |  | 28 | .0002 | 453 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 92.PETROLEUM ETHER 石油醚 | 8032-32-4 | E | E | E | E | >480 | .02 | ND | E | E | E | E | 126 | .002 | 12 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 93.PHENOL SAT. 酚 | 108-95-2 | NT |  |  |  | >480 | - | ND | E | E | E | E | >480 | .2 | ND | E | E | E | G | >480 | .06 | ND | NT |  |  |  | 32 | - | 78 |
| 94.PHOSPHORIC ACID 85% 磷酸 | 7664-38-2 | E | E | E | E | >480 | .04 | ND | E | E | E | E | >480 | .04 | ND | E | E | E | E | >480 | .04 | ND | E | E | E | E | >480 | .04 | ND |
| 95.POLYCHLORINATED BIPHENYLS(PCBS/50%)多氯聯苯 |  | NT |  |  |  | 343 | 1.0 | 216 | NT |  |  |  | >480 | 1.0 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 96.POTASSIUM HYDROXIDE 50% (KOH) 氫氧化鉀 | 1310-58-3 | E | E | E | E | >480 | .4 | ND | E | E | E | E | >480 | .3 | ND | E | E | E | E | >480 | .3 | ND | E | E | E | E | >480 | .4 | ND |
| 97.PYRIDINE 啶 | 110-86-1 | NT |  |  |  | NT |  |  | NT |  |  |  | 26 | - | 702 | NT |  |  |  | NT |  |  | NT |  |  |  | 1 | - | # |
| 98.RULE 66 SOLVENT 66號溶劑 |  | E | E | E | E | >480 | .001 | ND | E | E | E | E | 332 | .03 | 0 | NT |  |  |  | 9 | .002 | 126 | E | E | E | E | 42 | .02 | 60 |
| 99.SODIUM HYDROXIDE 50% (NaOH) 氫氧化鈉 | 1310-73-2 | E | E | E | E | >480 | .1 | ND | E | E | E | E | >480 | .1 | ND | E | E | E | E | >480 | .1 | ND | E | E | E | E | >480 | .04 | ND |
| 100.SULFURIC ACID 50% 硫酸 | 7664-93-9 | E | E | E | E | >480 | .04 | ND | E | E | E | E | >480 | .04 | ND | E | E | E | E | .480 | .1 | ND | E | E | E | E | >480 | .04 | ND |
| 101.1,1,2,2-TETRACHLOROETHANE 1,1,2,2-四氯乙烷 | 79-34-5 | NT |  |  |  | NT |  |  | NT |  |  |  | 18 | - | 1398 | NT |  |  |  | NT |  |  | NT |  |  |  | 6 | - | 2502 |
| 102.1,1,2,2-TETRACHLOROETHYLENE 1,1,2,2-四氯乙烯 | 127-18-4 | E | G | G | F | 373 | .0002 | 27 | NT |  |  |  | 28 | .0002 | 453 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 103.TETRAHYDROFURAN (THF) 四氫 喃 | 109-99-9 | G | P | P | P | 17 | .08 | 4026 | E | P | P | P | 11 | .08 | 4026 | NT |  |  |  | NT |  |  | NT |  |  |  | 1 | - | # |
| 104.TOLUENE (TOLUOL) 甲苯 | 108-88-3 | G | P | P | P | 28 | .002 | 150 | NT |  |  |  | 14 | - | 2256 | NT |  |  |  | NT |  |  | NT |  |  |  | 3 | - | 2100 |
| 105.TOLUENE DIISOCYANATE (TDI) 三異氰酸甲苯 | 584-84-9 | E | F | F | P | .480 | .3 | ND | NT |  |  |  | NT |  |  | E | E | G | F | >480 | .1 | ND | E | G | F | P | >480 | .06 | ND |
| 106.TOLUOL 甲苯 | 108-88-3 | G | P | P | P | 28 | .002 | 150 | NT |  |  |  | 14 | - | 2256 | NT |  |  |  | NT |  |  | NT |  |  |  | 3 | - | 2100 |
| 107.1,1,1-TRICHLOROETHANE 1,1,1-三氯乙烷 | 71-55-6 | F | P | P | P | 131 | .05 | 264 | F | P | P | P | 27 | - | 1182 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 108.TRICHLOROETHYLENE (TCE) 三氯乙烯 | 79-01-6 | P | P | P | P | 9 | .002 | 372 | NT |  |  |  | 11 | - | 3966 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 109.TRICHLOROTRIFLUOROETHANE 三氯三氟乙烷 | 76-13-1 | E | E | E | E | >480 | .01 | ND | E | E | E | E | >480 | .2 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | 11 | - | 192 |
| 110.TRIETHANOLAMINE (TEA) 三乙醇胺 | 102-71-6 | E | E | E | E | >480 | 5.0 | ND | E | E | E | E | >480 | 5.0 | ND | E | E | E | E | >480 | 5.0 | ND | E | E | E | E | >480 | 6.0 | ND |
| 111.TRIFLUOROETHANOL 三氟乙醇 | 75-89-8 | NT |  |  |  | NT |  |  | NT |  |  |  | >60 | - | ND | NT |  |  |  | NT |  |  | NT |  |  |  | 15 | - | 1302 |
| 112.TRIHYDROXYTRIETHYLAMINE 三 基三乙基胺 | 102-71-6 | E | E | E | E | >480 | 5.0 | ND | E | E | E | E | >480 | 5.0 | ND | E | E | E | E | >480 | 5.0 | ND | E | E | E | E | >480 | 6.0 | ND |
| 113. TURPENTINE 松節油 | 8006-64-2 | E | E | E | E | >480 | .0009 | ND | E | E | E | E | >480 | .02 | ND | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 114. VINYL ACETATE 乙酸乙烯酯 | 108-05-4 | E | F | F | F | 30 | .08 | 402 | E | E | G | G | 30 | .03 | 198 | NT |  |  |  | NT |  |  | NT |  |  |  | NT |  |  |
| 115.XYLENES (XYLOLS) 二甲苯 | 1330-20-7 | E | G | F | P | 92 | .002 | 24 | NT |  |  |  | 23 | - | 798 | NT |  |  |  | NT |  |  | NT |  |  |  | 4 | - | 1698 |
| 116.XYLOLS 二甲基苯酚 | 1330-20-7 | E | G | F | P | 92 | .002 | 24 | NT |  |  |  | 23 | - | 798 | NT |  |  |  | NT |  |  | NT |  |  |  | 4 | - | 1698 |

KEY TO DEGRADATION RATINGS:              KEY TO PERMEATION AND BREAKTHROUGH RATE:

| - (E) Excellent 0 to 10% - (G) Good 11 to 20% - (F) Fair 21 to 30% - (P) Poor over 30% | BTT-Breakthrough time (穿破時間) LDL-Lower detection limit (最低可測出值) PPM -Parts per million at breakthrough (百萬分之一) ug/CM2/MIN-Microgram per centimeter square per minute (浸透速率之單位) | ND-None Detected (未測出) >-Greater than (大於) <-Less than (小於) NT-No Tested (未測試) #-Rate too large to measure (速率大到無法測量) CAS# (美國化學文摘社化學品代號) |
| --- | --- | --- |

資料來源: 法國MAPA/ PIONEER 公司