| 手 套 材 質 物 理 特 性 表 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | PROPERTIES | NATURAL RUBBER | HYPALON | VITON | NEOPRENE |
| MECHANICAL PROPERTIES | HARDNESS RANGE (durometer A & D ) TENSILE STRENGTH, Mpa Pure gum Black loaded stocks SPECIFIC GRAVITY(Base Material) VULCANISING CHARACTERISTICS ADHESION TO METALS ADHESION TO FABRICS TEAR RESISTANCE ABRASION RESISTANCE COMPRESSION SET REBOUND Cold Hot | 30-90 A Over 20 Over 20 0,93 Excellent Excellent Excellent Good Excellent Good Excellent Excellent | 40-95 A Over 17 Over 20 1,12-1,28 Excellent Excellent Good Fair Excellent Fair Good Good | 55-95 A Over 12 Over 13 1,85 Good/Excellent Good/Excellent Good/Excellent Fair/Good Good Good/Excellent Good Excellent | 40-95 A Over 20 Over 20 1,23 Excellent Excellent Excellent Good Excellent Fair/Good Very Good Very Good |
| ELECTRICAL PROPERTIES | DIELECTRIC STRENGTH ELECTRICAL INSULATION | Excellent Good/Excellent | Excellent Good | Good Fair/Good | Good Fair/Good |
| FLUID RESISTANCE PROPERTIES | PERMEABILITY TO GASES ACID RESISTANCE Dilute Concentrated SOLVENT RESISTANCE Aliphatic hydrocarbons Aromatic hydrocarbons Oxygenated (ketones, etc.) Lacquer solvents RESISTANCE TO: Swelling in lubricating oil Oil and petrol Animal and vegetable oils Water absorption and/or hydrolytic stability | Fair Fair/Good Fair/Good Poor Poor Fair/Good Poor Poor Poor Poor/Good Very Good | Low/Very Low Excellent Very Good Good Fair Poor Poor Good/Excellent Good Good Very Good | Very Low Excellent Excellent Excellent Excellent Poor Poor Excellent Excellent Excellent Very Good | Low Excellent Good Good Fair Poor Poor Good Good Good Good |
| RESISTANCE TO ENVIRONMENTAL FACTORS | Oxidation Ozone Sunlight aging Heat ageing (upper limit cont. service) Flame* Heat Cold | Good Fair Poor 85OC Poor Good Excellent | Excellent Outstanding Outstanding 135OC Good Excellent Good | Outstanding Outstanding Outstanding 205OC Excellent Outstanding Fair/Good | Excellent Excellent Very Good 95OC Very Good Very Good Very Good |

Outstanding ﹕特佳  Excellent﹕佳  Good﹕好  Fair﹕尚可  Low﹕低  Very Low﹕很低

資料來源﹕美國杜邦ECUSTOMER部門

| 手 套 材 質 物 理 特 性 表 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 特 性 | NATURAL RUBBER | HYPALON | VITON | NEOPRENE |
| MECHANICAL PROPERTIES (機 械 特 性) | 硬度範圍 (durometer A & D ) Tensile strength抗拉力強度, Mpa Pure gum純膠 Black loaded stocks SPECIFIC GRAVITY(Base Material) 比重 VULCANISING 高溫及硫化處理 CHARACTERISTICS ADHESION TO METALS金屬附著力 ADHESION TO FABRICS布料附著力 TEAR RESISTANCE抗撕裂性 ABRASION RESISTANCE耐磨擦力 COMPRESSION SET壓縮設定 REBOUND 回復性 Cold冷 Hot熱 | 30-90 A Over 20 Over 20 0,93 Excellent Excellent Excellent Good Excellent Good Excellent Excellent | 40-95 A Over 17 Over 20 1,12-1,28 Excellent Excellent Good Fair Excellent Fair Good Good | 55-95 A Over 12 Over 13 1,85 Good/Excellent Good/Excellent Good/Excellent Fair/Good Good Good/Excellent Good Excellent | 40-95 A Over 20 Over 20 1,23 Excellent Excellent Excellent Good Excellent Fair/Good Very Good Very Good |
| ELECTRICAL PROPERTIES | DIELECTRIC STRENGT耐電壓強度 ELECTRICAL INSULATION 絕緣性 | Excellent Good/Excellent | Excellent Good | Good Fair/Good | Good Fair/Good |
| FLUID RESISTANCE PROPERTIES(防 液 體 特 性) | PERMEABILITY TO GASES 氣體滲透性 ACID RESISTANCE 耐酸性 Dilute稀釋 Concentrated 濃縮 SOLVENT RESISTANCE 耐溶劑 Aliphatic hydrocarbons Aromatic hydrocarbons Oxygenated (ketones, etc.) Lacquer solvents RESISTANCE TO: Swelling in lubricating oil 潤滑油 Oil and petrol 油與石油 Animal and vegetable oils 動物性及 植物性油脂 Water absorption and/or 吸水力 hydrolytic stability 水解安定性 | Fair Fair/Good Fair/Good Poor Poor Fair/Good Poor Poor Poor Poor/Good Very Good | Low/Very Low Excellent Very Good Good Fair Poor Poor Good/Excellent Good Good Very Good | Very Low Excellent Excellent Excellent Excellent Poor Poor Excellent Excellent Excellent Very Good | Low Excellent Good Good Fair Poor Poor Good Good Good Good |
| RESISTANCE TO (抗環境因子) # ENVIRONMENTAL FACTORS | Oxidation 氧化 Ozone 臭氧 Sunlight aging 日曬 折舊 Heat aging 受熱折舊 (upper limit cont. service) Flame*火燄 Heat 熱 Cold 冷 | Good Fair Poor 85OC Poor Good Excellent | Excellent Outstanding Outstanding 135OC Good Excellent Good | Outstanding Outstanding Outstanding 205OC Excellent Outstanding Fair/Good | Excellent Excellent Very Good 95OC Very Good Very Good Very Good |

Outstanding :特佳  Excellent:佳  Good:好  Fair:尚可  Low:低  Very Low:很低 資料來源:美國杜邦ECUSTOMER部門